Description TRFS Sheild  WD is a two-component water dispersed epoxy floor coating for use on concrete and polymer modified cementitious screeds. TRFS Sheild  WD is designed to provide a tough, hard wearing protective floor finish in a range of colours. Being water-based, TRFS Sheild  WD may also be applied to 7 day old ‘green’ concrete. Its easy to clean, silk finish makes the product ideal for garages, food and beverage industries, light industrial units, warehouse floors and other areas subject to pedestrian and light vehicular traffic.

# Appearance

Semi-gloss / silk finish available in a wide range of colours and clear.

# Features & Benefits

- Water based technology

- Resistant to general chemical spillages

- Durable and non-dusting

- Economical and easy to apply  Thickness  Approximately 250 microns wet film thickness from two coats (approximately 125 microns dry film thickness).

Finished floor * Over coating period 8 - 24 hours Cure time to light pedestrian traffic 24 hours Cure time to medium duty traffic 48 - 72 hours Full cure 7 days

The material should be protected from contact with water for 7 days.

* The above cure times are approximate and given as a guide only. These times can vary due to prevailing site conditions. At lower temperatures curing times will be extended.

Pack Size

5 kg and 10 kg units

Coverage*

A minimum of two coats are required. Some substrates may require additional coats depending on profile and porosity. Light or bright colours such as safety yellow or safety red may require additional coats to achieve full opacity. As a guide, a medium quality substrate may achieve 4 m2/kg from 2 coats and a more porous substrate may achieve 3 m2/kg from 2 coats.

* Coverage figures given are theoretical. Practical coverage rates may vary due to wastage factors and the type, condition, profile and porosity of the substrate.

Colours TRFS Sheild  WD is not 100% colour fast and may yellow over time. The rate of change will depend on UV light and heat levels and cannot be predicted. This will be more pronounced with lighter colours and blue shades and does not compromise the product’s performance or chemical resistance characteristics.

# Application Conditions

Resin products should not be mixed and laid outside of the range 10 °C to 25 °C. Localised heating or cooling equipment may be required outside this range to achieve ideal temperature conditions. To reduce the risk of “blooming” caused by condensation, the climate above the uncured floor should be maintained at least 3 °C above the dew point for at least 48 hours after application. The atmospheric relative humidity should be below 80% and good ventilation should be provided to aid the removal of water and maintain curing times. The substrate should be surface dry with a maximum relative humidity of 80% and free from rising damp and ground water pressure.

# Typical Properties, 28 days at 20 oC

BS 8204-6 Adhesion to concrete (BS EN 1504-2) (concrete failure)

# Type 1/2 > 1.5 MPa

The typical physical properties given above are derived from testing in a controlled laboratory environment. Results derived from testing field- applied samples may vary dependent upon site conditions.

Cure Schedule at 20 oC

Working life of full packs *

* Usable working life of material spreading as per the application instructions.

# 1 hour

mixing and immediate

TRFS Sheild  WD does not have a visible end of pot-life. After the pot life has expired the material will not be hardened or have increased in viscosity but the characteristics of the product will have changed and the final properties of the coating will be affected. Discard excess material after this period.

f